Efficacious Remediation of Methylene Blue (MB) and Crystal Violet (CV) from the Aquatic Environment by Using Magnetic Hydrogel Halloysite Nanotubes

Leila Choopani1, Mohammad Mehdi Salehi1, Reza Eivazzadeh-Keihan*, Ali Maleki*

Catalysts and Organic Synthesis Research Laboratory, Department of Chemistry, Iran University of Science and Technology, Tehran 16846-13114, Iran.

*Corresponding authors. E-mail: reza_eivazzadeh@alumni.iust.ac.ir (Reza Eivazzadeh-Keihan), E-mail: maleki@iust.ac.ir (A. Maleki) Fax: +98-21-73021584; Tel: +98-21-7322831.

1 These authors contributed equally.

Author’s ORCIDs:

Mohammad Mehdi Salehi: https://orcid.org/0000-0003-3648-1865

Ali Maleki: https://orcid.org/0000-0001-5490-3350

| Content | Page |
| --- | --- |
| Table S1. All materials used in this research have been marked and are pure. | S2 |
| Table S2. A description of the equipment used in this study. | S3 |
| Table S3. The Surface area, Pore volume and Pore size of Ge/Pec-HNTs and Ge/Pec-HNTs@IONP magnetic hydrogel halloysite nanotubes. | S4 |
| Table S4. Adsorption of MB and CV on the Ge/Pec-HNTs@IONP magnetic hydrogel halloysite nanotubes: isotherm, kinetic, and correlation coefficients. | S5 |
| Figure S1. Chemical structure of )a) MB, and )b) CV. | S6 |
| Figure S2. The standard Calibration curve for determining Methylene blue Concentration in aqueous solution. | S7 |
| Figure S3. The standard Calibration curve for determining Crystal Violet Concentration in aqueous solution. | S8 |
| Figure S4. Reusability of the Ge/Pec-HNTs@IONP magnetic hydrogel halloysite nanotubes (a) adsorption and (b) desorption percentages of MB and CV during two cycles. | S9 |
| Figure S5. The suggested mechanism for adsorption of MB and CV by the Ge/Pec-HNTs@IONP magnetic hydrogel halloysite nanotubes. | S10 |

Table S1. All materials used in this research have been marked and are pure.

| Material | Brand and Purity |
| --- | --- |
| Pectin (Pe) | Sigma-Aldrich, CAS Number (9000-69-5) |
| Gelatin (Ge) | Sigma-Aldrich, CAS Number (9000-70-8) |
| Halloysite nanotubes (HNTs) | Sigma-Aldrich, CAS Number (1332-58-7) |
| Glutaraldehyde | Sigma-Aldrich, CAS Number (111-30-8) |
| Sulfuric acid | ACS reagent, 95.0-98.0%, Sigma-Aldrich |
| Methylene Blue (MB) | Sigma-Aldrich, CAS Number (61-73-4) |
| Crystal Violet (CV) | Sigma-Aldrich, CAS Number (548-62-9) |
| Ferric chloride hexahydrate (FeCl3·6H2O) | ACS reagent, 97% |
| # Ferrous chloride tetrahydrate (FeCl2·4H2O) | Reagent Plus®, 98%, Sigma-Aldrich |
| Ammonia | Puriss, anhydrous, ≥99.9%, Sigma-Aldrich |
| Sodium hydroxide (NaOH) | Reagent grade, ≥98%, pellets (anhydrous), Sigma-Aldrich |
| Hydrochloric acid (HCL) | ACS reagent, 37% |
| Ethanol | Sigma Aldrich (96%) |

Table S2. A description of the equipment used in this study.

| Equipment | Brand and model |
| --- | --- |
| FTIR spectroscopy | Shimadzu FT-IR-8400S |
| XRD | DRON-8 X-ray diffractometer |
| FESEM | KYKY-EM8000F |
| EDX spectroscopy | VEGA-TESCAN-XMU |
| TGA analysis | Bahr-STA 504 |
| VSM | Kavir’s LBKFB (Kashan, Iran) |
| BET | Micromeritics ASAP 2010 |
| liquid UV analysis | Shimadzu UV-2550 |
| Thermometer | Fluke (572-2 infrared) |
| pH Meters | PHS-3C pH |
| Oven | Genlab Ltd |
| Filter paper | Whatman (grade 602h, Particle retention < 2µm) |

Table S3. The Surface area, Pore volume and Pore size of Ge/Pec-HNTs and Ge/Pec-HNTs@IONP magnetic hydrogel halloysite nanotubes.

| Sample | Surface areaa (m2.g-1) | Pore volumeb (cm3.g-1) | Pore sizeb (nm) |
| --- | --- | --- | --- |
| Ge/Pec-HNTs | 7.377 | 0.0064 | 3.514 |
| Ge/Pec-HNTs@IONP | 35.244 | 0.0690 | 7.832 |

a: By using BET analysis, the surface area parameter was obtained.

b: Through BJH analysis, the pore volume and size characteristics were obtained.

Table S4. Adsorption of MB and CV on the Ge/Pec-HNTs@IONP magnetic hydrogel halloysite nanotubes: isotherm, kinetic, and correlation coefficients.

| Model |  | Parameters | MB | CV |
| --- | --- | --- | --- | --- |
| Isotherm | Freundlich | KF, mg.g-1 | 74.671 | 213.13 |
|  |  | n | 2.211 | 1.764 |
|  |  | R2 | 0.9629 | 0.9950 |
|  | Langmuir | Qmax (mg/g) | 434.783 | 666.667 |
|  |  | KL (L/mg) | 0.11917 | 0.55556 |
|  |  | R2 | 0.9606 | 0.9957 |
| Kinetics | Pseudo-first-order (PFO) | K1 (min-1) | 0.0755 | 0.0124 |
|  |  | Qe, experimental (mg/g) | 208.684 | 241.955 |
|  |  | Qe calculated (mg/g) | 65.157 | 15.602 |
|  |  | R2 | 0.988 | 0.9485 |
|  | Pseudo-second-order (PSO) | k2 (min-1) | 0.00320 | 0.00569 |
|  |  | Qe, experimental (mg/g) | 208.684 | 241.955 |
|  |  | Qe calculated (mg/g) | 222.222 | 243.902 |
|  |  | R2 | 0.9961 | 0.9992 |

Figure S1. Chemical structure of )a) MB, and )b) CV.

Figure S2. The standard Calibration curve for determining Methylene blue Concentration in aqueous solution.

Figure S3. The standard Calibration curve for determining Crystal Violet Concentration in aqueous solution.

Figure S4. Reusability of the Ge/Pec-HNTs@IONP magnetic hydrogel halloysite nanotubes (a) adsorption and (b) desorption percentages of MB and CV during two cycles.